[image: image1.jpg]' BAbRRhACH INA'S




TECHNICAL INFORMATION

10. ECO-CREAMS

10.2 TO-BE-POLISHED ECO-CREAMS

10.2.14. ECO-CREMA STAIN WAX 
CHARACTERISTICS:  

Mixture of acrylic polymers, waxes and natural oils in an aqueous medium. A natural shine and excellent penetration are achieved. It is resistant to water droplets and color migration.
Specifically designed for synthetic material.
APPLICATION FIELD:  

Crust leathers and synthetic material that you want to finish on the last itself and thus present a shoe customized to the manufacturer's taste.  Keep in mind that the leather should be as bare as possible so that the cream can be absorbed as easily as possible and thus achieve the desired finish.
INSTRUCIONS FOR USE:  

Apply the ECO CREMA STAIN WAX with a suitable sponge of great resistance, high density, with very small and soft cells. trying to reach all corners, it is preferable to apply the cream on a last to be able to access the entire surface of the leather or synthetic material . Let it dry for at least 4-6 minutes, depending on the ambient temperature and humidity,  Then brush with a horsehair brush or cloth at approximately 500/800 rpm, trying to distribute the wax evenly. Apply a top coat and finally brush with a cotton or wool brush soaked in polishing wax at approximately 500-800 rpm to achieve the desired shine and feel.. It is advisable and recommended to apply this ECO CREMA STAIN WAX in good ventilation and protection conditions on the hands to avoid contact with the skin, thus avoiding any allergic reaction.
SECURITY:  

Look up the general security section.
REMARKS:  
Our zone laboratories will supply you with any coloured ECO-CREMA STAIN WAX.  
Barrachinas cannot control the conditions under which its products are used, therefore do not accept responsibilities concerning the results and/or consequences from its usage.







DATA OF REVIEW: 21/07/25 (1)
